Polyurethane Softenert DPU

DPU is a new thermo-reactive polyurethane for fast drying, very full and extremely soft handle on cellulosic and polyamide fibres. Applied with silicone softeners, Sandoperm RPU Liquid produces a hydrophilic finish, improving the elasticity/shape recovery of knitted goods .

[Properties]

- Appearance: transparent liquid

- Chemical character: polyurethane resin

- Ionicity: noninoic

- PH value: 6-7

- Solubility: soluble in water

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Produces a very washfast, very full and soft handle.

- Improves the crease recovery angle and wash and wear behavior in combination with crosslinking agents for cellulosic fibres.

- Improves the elasticity and shape recovery of knitted fabrics.

- Produces hydrophilic finishing effect.

[Applications]

Examples of use

Woven fabric handle finishing

20-40g/l   DPU

pad, dry  at 120℃ ,and cure at 170℃

Woven fabric resin finishing

60g/l  Resin NFD

18g/l  Cat.  CS-200

20g/l  DPU

20g/l  DT-5258

pad, dry and cure at 150℃ for 3 minutes.

[packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.