Stiffening Agent YT-20

Stiffening agent YT-20 is a handle modifier with durable effect .Fabrics finished by it have good stiffness.

[Properties]

- Appearance: white , low viscosity dispersion

- Chemical character: acrylate copolymer dispersion, self-crosslinking

- Ionicity:  anionic

- PH value: 6±0.5 (1% aqueous solution)

- Solubility: soluble in water

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Hard , somewhat elastic handle.

- Resistant to mild machine washing and dry cleaning.

[Applications]

Stiffening agent YT-20 can be applied by padding , face padding, doctor coating and foam application methods. It is especially suitable for the finishing and bonding nonwovens and woven fabrics by all known methods and for handle modification in resin finishing.

Examples of use

Woven fabric finishing

20-100g/l   YT-20

pad, dry and cure at 150℃

[Packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.